# DATA SHEET

Premier

PVC Ceiling Panel.

Product: Open-cell tongue and groove panel in PVC.

Characteristics: Premier panels are impervious to moisture, extremely resistant to chemicals and will not rot or support mould. The panels exhibit good sound and thermal insulation properties, and are UV stabilised to prevent fading in sunlight.

Fire safety: Premier Panels conform to BS 476 Part 7 Class ‘1’.

(BS476 Part 6 Class ‘0’ when fitted to a non-combustible substrate)

Purpose: Premier Panels are specifically designed as a low maintenance finish for interior walls and ceilings in areas where appearance, hygiene and cleanliness are of extreme importance.

#### Design Data

| Nominal | Colour | Size | Finish |
| --- | --- | --- | --- |
| Panel Thickness |  |  |  |
| 9mm | Various | 250mm x 3-6m | Matt |

##### Physical Properties

| Property | Typical Value | Test Method |
| --- | --- | --- |
| Density | 1.5g/cm3 | DIN 53479 / ISO 1183 |
| Tensile Strength | 55N/mm2 | DIN 53455 / ISO 527 |
| Elasticity Modulus | 2800N/mm2 | DIN 53457 / ISO 53455 |
| Impact Resistance | No break | DIN 53453 / ISO 179 |
| Shore Hardness | D83 | DIN 53505 / ISO 868 |
| Vicat Softening Point | 83(c | DIN 53460 / ISO 306 |
| Highest Application Temp. | 60(c | ISO 75 |
| Thermal Expansion Coeff. | 0.06mm/m(c | DIN 52328 |
| Surface Resistance Thermal Conductivity | Ca 10E13 Ohm 0.15 W/m(c | DIN 53482 DIN 52612 |